Microwave Bonding of Polymer-Based Substrates

for Potential Encapsulated Micro/Nano Fluidic Device Fabrication

Kin Fong Lei 1, Syed Ahsan2, Nasser Budraa2, Wen J. Li 1,*, and John D. Mai 2

1 Centre for Micro and Nano Systems, The Chinese University of Hong Kong, HKSAR

2 Microwave Bonding Instruments, Inc., Altadena, USA

* E-mail: wen@acae.cuhk.edu.hk    Phone: +852 26098475	Fax: +852 26036002

ABSTRACT Microwave-based bonding of polymer substrates is presented in this paper to illustrate a promising technique for achieving precise, localized, low temperature bonding. Microwave power can absorbed by a very thin film metal layer deposited on a polymer (PMMA) substrate surface. The intense thin-film volumetric heating promotes localized melting of refractory metals such as gold. One of the advantages of the process is that PMMA is relatively transparent to microwave energy in the 2.4 GHz regime. This makes it an excellent substrate material for microwave bonding. Selective heating and melting of the thin layers of metal also causes localized melting of the PMMA substrates and improves adhesion at the interface. We have shown that ~1 (m of interfacial layer can be generated that is composed of the melted gold and PMMA, and which can hold two substrates together under applied tension greater than 100 lb/in2 (7 kg/cm2). We also used lithographically patterned metal lines on a PMMA substrate to demonstrate that the PMMA remains optically transparent after microwave processing. A numerical simulation was also performed and validated with experimental results to show that globally the PMMA substrates indeed remained below its melting point during the microwave bonding process. The novel bonding process will open up possibilities for precise and total encapsulation of polymer-based micro/nano fluid devices – which are impossible to built using existing polymer bonding techniques. Keywords: Microwave Bonding, Polymer Substrates Bonding, Microfluidic Devices, Nanofluidic Devices

###### INTRODUCTION

Since the publication of results from silicon die microwave bonding experiments at the Jet Propulsion Laboratory (JPL) [1] in 1999, there has been interest in selective heating for MEMS applications using electromagnetic energies at frequencies from radio frequency (RF) up to microwaves. A group from the University of Wisconsin [2] showed that direct silicon wafer bonding, which usually requires temperatures greater than 1000 (C, was possible using a 2.45 GHz microwave source with a power output of 1500 W. Complete, void free bonding was achieved using this process in less than 5 minutes. Similarly, a group from the University of Minnesota [3] used RF heating to bond silicon wafers together via a dielectric insulator interface. This group applied 500 W of power from a 14 MHz source for 7 minutes below 280 (C to bond silicon wafers via a 2 to 20 (m thick polyimide dielectric layer. Other groups have attempted sealing using compression waves at ultrasonic frequencies to get hermetic sealing, similar to that achieved by the JPL group using electromagnetism. One group from UC Berkeley [4] used ultrasonic frequencies at up to 25 W for almost 2 seconds to bond approximately 2 mm2 of In/Au and up to 50 W for 5 seconds to bond approximately 2 mm2 of Al/Al. However, until now, there has not been much focused attention on using selective microwave heating to join thin film metal layers between polymer substrates.

In recent years, polymer-based micro fluidic devices have become increasingly important in biological applications [5]. However, polymer substrates must be bonded to make functional micro channels, and adhesion between the substrates is a problem of great practical concern.  Existing polymer-to-polymer substrate bonding methods includes thermal-compression, ultrasonic, or gluing by application of either epoxy or methanol. Unfortunately, these techniques are not precise when compared to standard IC/MEMS bonding processes, i.e., they may induce global and localized geometric deformation of the substrates or leave an interfacial layer with significant thickness variation.  For channels in the millimeter to a few hundred microns range, these drawbacks are tolerable. However, it is implausible to construct micron and nanometer sized channels using these techniques since significant global and local material deformations may distort the micro/nano channel geometries.

In this paper we will present our ongoing work to use localized microwave heating to bond polymer (PMMA) substrates without causing any global deformation to the substrates and resulting in a precise and well-controlled interfacial layer thickness of 1(m.  Thus far, we have shown that microwave energy can be used to selectively melt a film as thin as 50nm of gold deposited on each side of the two PMMA substrates to be bonded. Melting of these thin layers of gold caused localized melting of the PMMA substrates and allowed them to bond.  The 1 (m interconnect layer is composed of the melted gold and PMMA and has been shown to hold the substrates together under applied pressure greater than 100 lb/in2 (7 kg/cm2).

###### MICROWAVE BONDING

The central idea behind microwave bonding is to use the nature of the interaction of high frequency energies with thin film metals that are used as bonding interfacial layers in a single mode cavity (SMC). In such a cavity the power delivered to metal contact is proportional to the conductivity and the electric field (E2), as shown in Equation (1) [6]. In Equation (1), (o is the fundamental frequency, (o is the permittivity of free space, (’ is the real component of the material dielectric permittivity and tan( is the loss tangent of the material.

(1)

In microwave bonding, most of the power is delivered through a microwave transparent substrate and is absorbed by a very thin-film metal of less than one micron thick (skin depth). This power induces heating that leads to high temperature melting of refractory metals such as gold. The low electrical conductivity of a polymer or semiconductor substrate, relative to a metal, allows the substrate to essentially remain unaffected by the energy deposited in the SMC. The high intensity fields found in a SMC is unique to these types of cavities and allows the melting of high-melting-temperature thin films or contact points as found in this application. The thinness of the metal (skin depth), the high intensity, and the short application time contribute to the following critical advantages:

1.  Localized power concentration allows for strong hermetically bonded areas between the substrates. High bond strength results from the utilization of high melting temperature metals at the interface. This means higher device reliability.

2. Selective heating of the thin metal means the bonding process is a globally low-temperature process. The temperature of bulk substrate is less then 100 (C, which is lower than the melting point of the bond metal; this means a polymer with a low-melting temperature could be used as a substrate. Also, since the substrate temperatures remains low, adverse thermal coefficient of expansion mismatches are minimized.

3. Unlike some laser welding and ultrasonic bonding techniques, the process is low cost because the bonding occurs simultaneously and quickly.

###### MICROWAVE BONDING TO POLYMER

In general, we succeeded in bonding PMMA to silicon and PMMA to PMMA substrates together using selected microwave frequencies to locally melt the interface metallic thin films between the substrates. As shown in Figure 1, the prototype equipment is capable of handling test dies up to 45 mm in diameter.

Our bonding experiments showed that PMMA is relatively transparent to microwave energy near the 2.4 GHz frequency band. This makes PMMA an excellent material for microwave bonding. Most of the microwave energy is absorbed by the thin film metals at the interface, thus minimizing heating in the bulk PMMA substrate. An oscilloscope was attached to a diode antenna that measures the amplitude of the resonance peak in the microwave processing chamber as the frequency was swept from 2.3 to 2.5 GHz. Data captured from an oscilloscope is shown in Figure 2. The resonant peak of the empty chamber is shown in Figure 2a. The resonant peak of the chamber loaded with 2 sample blocks of PMMA is shown in Figure 2b. The y-axis is the measured output voltage in milli-volts. We found a maximum reduction in the value of the resonant peak between the loaded and empty chamber configurations of less than 1%. This shows PMMA essentially transparent to microwave energy.

Figure 1. The prototype of the microwave bonding equipment.  The current design allows up to 45 mm in diameter sample to be fitted in to the sample holder.

Figure 2. Resonant peak in the microwave-processing chamber as the frequency is swept from 2.3 to 2.5 GHz (a) Empty chamber. (b) PMMA loaded chamber. The x-axis presents time-sequenced data. The y-axis is the measured output voltage in milli-volts.

###### EXPERIMENTAL RESULT

A. Silicon to PMMA Bonding

Silicon to PMMA bonding was achieved by using thin film 63% Sn and 37% Pb solder pre-forms to address the problem of PMMA substrate flatness, as shown in Figure 3. The thickness of silicon and PMMA is 1 mm and 3 mm, respectively. A 500 Å Cr adhesion layer and 500 Å Au bonding layer were e-beam evaporated onto both surfaces. The pre-form is 50 (m thick and melts at 183(C. Microwave bonding of PMMA to a silicon die is shown in Figure 4. This was done at approximately 30 W of applied power for 180 seconds. Note the critical fact that the Au surface of the PMMA was unaffected (by visual examination) after processing and the bulk PMMA was still transparent. It was possible to look through the backside of the PMMA to see the unaffected Au top layer.

Figure 3.  Illustration of die stack for Au covered silicon and Au covered PMMA bonding experiment. Solder pre-form films of 63% Sn and 37% Pb were used to enhance PMMA-Si bonding.

Figure 4. PMMA to silicon bond.  Note, the apparent bottom Si substrate is a reflection of the top Si substrate off the Au film on PMMA substrate.

B. PMMA to PMMA Bonding

Embossed PMMA and PMMA bonding is possible via thin film Au already deposited on the surface, as shown in Figure 5. Using hot embossing technique [5], microchannel can be created on the PMMA. A 500 Å Cr adhesion layer and a 500 Å Au bonding layer were e-beam deposited onto both embossed PMMA and bare PMMA surface. An example of two PMMA substrates successfully bonded together is shown in Figure 6. Two substrates were bonded at 10 W for approximately 120 seconds. Again, the substrates were not affected based on visual examination after the microwave bonding processing.

Figure 5. Illustration showing the dimensions of the PMMA substrates and Au thin film layers used in the PMMA-PMMA bonding experiment.

An SEM image of the cross section of the PMMA-PMMA substrates is shown in Figure 7. As shown in the figure, the thickness of the interfacial layer is approximately 1 (m and is a precise and well-controlled layer. From the EDX spectra, as shown in Figure 7b and 7c, the interfacial layer composes of the mixture of Au and carbon, which indicates that the microwave energy melted the Au layer causing localized melting of the PMMA substrates to be bonded. This bond was shown to hold the substrates together under applied tension greater than 100 lb/in2 (7 kg/cm2).

Figure 6. Embossed PMMA to bare PMMA bond.

Figure 7. (a) SEM image of PMMA to PMMA bonding interface. (b) EDX spectra of interface region showing that it mainly composes of Au. (c) EDX spectra of PMMA, showing that it is mostly carbon.

C.  Si-In to Au-PMMA Bonding

We have also successfully bonded PMMA substrates with patterned Au layers to Si substrates with patterned In layers.  The Si substrates are 1 cm x 1 cm x 400 (m thick, lightly doped silicon covered with patterned thin film layers of 300 Å Cr / 1000 Å Au and 2 (m In. The PMMA substrates are 2 mm thick with patterned thin film layers of 500 Å Au / 500 Å Cr.  Samples were bonded using less than 5W of power processed for exactly 45 seconds.  An example of bonded substrates is shown in Figure 8.

IR measurements, as shown in Figure 9, were carried out in real-time during the bonding process of 20W power in 5 seconds to study the temperature distribution on the bonding substrates . In general, we found that some parts of the bonding substrates reached 70(C, which is below the melting temperature of PMMA, but the bulk of the bonding substrates remained near room temperature. After the microwave bonding process, the transparency of bulk PMMA was not changed and there was no global deformation to the substrates.

Figure 8. An example if Si-In to Au-PMMA bond. Note that the PMMA is still transparent after the bond and the Au “rings” are still clearly defined. This proves that microwave bonding affects only the interfacial metal layer and will not globally heat the PMMA substrate.

Figure 9. IR image of PMMA stack in the microwave chamber after 20W of power is applied for 5 seconds. Note that edges are heated (darker shade), possibly caused by IR emission from gold visible on the sides of the sample due to misalignment; IR reflection from the sides of the sample holder tube is also visible. Clearly, the center body of the PMMA stack is near room temperature (stripes).

HEAT TRANSFER NUMERICAL SIMULATION

A thermal-dynamical 2-D, time dependent simulation was performed using a finite element method solver to provide insight into the heat transfer mechanism during the microwave bonding process. The 2-D heat transfer equation solved is:

(2)

here is the density of the material, C, the specific heat, k, the thermal conductivity, T, the temperature at a point inside the material, h, the convective heat coefficient, Ta, the ambient temperature, and Q is generated heat density.

In the simulation, the three main structural layers are silicon, PMMA and gold as illustrated in Figure 10.  The gold metallization is locally and volumetrically heated via microwave processing techniques. Heat is generated mainly inside the gold layer. The microwave power is dissipated uniformly inside the gold layer. This heat is transferred to PMMA and silicon by thermal conduction. The heat from the surface is dissipated to the surroundings by convection and radiation.

Figure 10. Illustration showing the subtrate and thin film used in the heat transfer simulation.

As the sample is symmetrical in length, only half of the sample was simulated. The thickness of silicon and PMMA layers used were 1 mm and 3 mm, respectively, and the total gold layer thickness was 0.2 (m.  The convective heat transfer coefficient at the boundary of the sample, h, is 3 W/m2K, based on previous experimental and simulated results with other silicon die stack combinations.  Heat transfer through radiation was also taken into consideration.  In order to accurately model the existence of thermal impedance at interlayer boundaries, two artificial junction layers are added to the simulation.  They represent the omnipresence of surface irregularities between the layers leading to a lower thermal conductivity than an ideal case, allowing the model to better approximate measured data and reality. One layer (25 (m thick) is between the silicon and the gold and the other layer (75 (m thick) is between the gold and the PMMA. Both layers were given a thermal conductivity of 0.05 W/m-K.A summary of the relevant physical parameters used for the materials in the simulation is given in Table 1.

Table 1. Properties used to model the structural layer in the simulation.

|  | Density (Kg/m3) | Specific Heat (J/Kg-K) | Thermal Conductivity (W/m-K) |
| --- | --- | --- | --- |
| Silicon | 2333 | 700 | 142 |
| Gold | 19300 | 128 | 320 |
| PMMA | 930 | 2386 | 0. 217 |

As shown in Figure 11, the experimental heating profile (in solid line) and numerical simulation (in dotted line) match well for the given power input and heating time (35 seconds).  The experimental data was taken by a pyrometer targeted at the top silicon surface of the stack inside of the microwave cavity during processing. This measured temperature serves as one boundary condition for the simulation, and it should be noted that this measured temperature is an average value due to the fact that the IR transparency of silicon is temperature dependant.  All temperature is in degrees Kelvin.  In this simulation, a Q of 4.05 x 109 W/m3   was input to match the experimental power input, and the physical requirement that the melting point of indium was reached. Figure 12 shows the centerline temperature profile at various times during the 35 seconds that power is applied. Along the x-axis, at x = 0 corresponds to the bottom of the PMMA layer.  Due to the high thermal conductivity of silicon, the temperature at x = 3 (the approximate thin film interface location in Figure 12) and x = 4 (the top of the silicon layer) is almost identical at any instant in the simulation.  The centerline position is illustrated by the vertical line through the die stack in Figure 12.

Figure 11. Temperature (K, vertical axis) versus time (seconds, horizontal axis) profile of top surface of the silicon as power is being applied.

Figure 12. PMMA and silicon die stack centerline temperature (K) profile at different times during heating.

Based on the close match with the experimental data at the top silicon surface, we argued that these calculated internal centerline values accurately measure the internal temperature distribution of the stack.  Thus, although the temperature at the metal layer (x = 3) is high enough to melt any indium or solder preforms that may be inserted during the physical bonding experiments, the PMMA temperature (0<x<3 in Figure 12) remains below its melting point due to the localized heating advantages of microwave processing.  The simulated spatial temperature distribution of the Si-Au-PMMA bond at this time is shown in Figure 13.  As shown, most of the PMMA layer is below its melting point, with an average bulk temperature around 380K.  This reinforces the conclusion that microwave thermal processing can be used for bonding of metals and PMMA without global deformation of the PMMA substrate, i.e., heating only occurs locally near the bonding metal layer between the substrates.

Figure 13. Simulation result at time = 35 seconds. Temperature distribution across the entire die stack immediately before the input power is turned off. (x-axis and y axis are distance in meters).

FUTURE WORK

We have already demonstrated that it is possible to produce micro/nano structure using micro molding technique [7], as shown in Figure 14. It includes mastering and replication processes. In the mastering process, a molding master is fabricated by lithography and electroforming. After obtaining the molding master, the micro/nano structures on the molding master can be transferred to a polymer substrate by a hot embossing machine. However, none of the existing bonding techniques, such as thermal-compression, ultrasonic, or gluing, would allow us to seal them. From the above initial microwave bonding results, we have proved that microwave bonding can be used to bond polymer substrates to Si or other polymer substrates. So, our ongoing work is to use microwave bonding technique to seal the micro cavities by lithographically patterned metal lines around the cavities and bond them with a flat substrate. We will shortly report our experimental results on this process elsewhere.

CONCLUSIONS

A low temperature bonding technique for polymer-based substrates to achieve a precise and well-controlled bonding interfacial layer has been described. These initial results indicate that microwave bonding has great advantages over thermal-compression and other conventional polymer to polymer bonding techniques, especially when micro/nano structure is to be encapsulated. For micro/nano fluidic applications, microwave bonding will give much advantage for bonding polymer substrates to make functional devices.

Figure 14. (a) Scanning Probe Microscope (SPM) image of a molded PMMA substrate with nano-cavities. The cavities have dimensions of width ~680 nm, depth ~200nm, and lengths of  ~1.08 (m, ~2.19 (m, and ~3.88 (m, respectively. (b) AFM image of a micro channel made by compact disc based injection molding process. The dimension is 51.9 (m in width, 283.2 nm in depth.

References

[1]	Nasser Budraa, H. W. Jackson, M. Barmatz, William T. Pike, and John D. Mai, “Low Pressure and Low Temperature Hermetic Wafer Bonding using Microwave Heating”, IEEE MEMS 1999, pp. 490-492, Orlando Florida, January 17-21, 1999.

[2]	Keith Thompson, Yogesh Gianchandani, John Booske, and Reid Cooper, “Si-Si Bonding Using RF and Microwave Radiation”, pp. 226-229, Transducers 2001.

[3]	Andrey Bayrashev, and Babak Ziaie, “Silicon Wafer Bonding with an Insulator Interlayer Using RF Dielectric Heating”, IEEE MEMS 2002, pp. 419-422, Las Vegas, NV, January 20-24, 2002.

[4]	Jongbaeg Kim, Mu Chiao, and Liwei Lin, “Ultrasonic Bonding of In/Au and Al/Al for Hermetic Sealing of MEMS Packaging”, IEEE MEMS 2002, pp.415-418, Las Vegas, NV, January 20-24, 2002.

[5]	Gwo-Bin Lee, Shu-Hui Chen, Guan-Ruey Huang, Wang-Chou Sung, and Yen-Heng Lin, “Microfabricated Plastic Chips by Hot Embossing Methods and Their Applications for DNA Separation and Detection”, Sensors and Actuators B 75, pp. 142-148, 2001.

[6]	A. F. Harvey, Microwave Engineering, pp.247-252, Academic Press, New York, 1963.

[7]	Victor K. W. Li Chong, K. F. Lei, Wen J. Li, and Thomas Y. S. Lee, “Development of Mass-Manufacturable Micro/Nano Fluidic Devices Using Standard CD Fabrication Technology”, IMU2 2003, Taiwan, 2003.

Biography

| Kin Fong Lei received his M.Phil. degree in Mechanical and Automation Engineering from The Chinese University of Hong Kong (CUHK) in 2000. His research interest is in microfluidic device, micro total |  |
| --- | --- |
| analysis system, and bio-engineering. Currently he is a Ph.D. candidate in Automation and Computer-Aided Engineering at CUHK. |

| Syed Ahsan received his M.S. degree in Electrical Engineering from the University of California at Los Angeles (UCLA) in 2003. From 2000 to 2003 he worked as a graduate researcher in the Integrated Photonics Laboratory, |  |
| --- | --- |
| UCLA. His graduate research work was on modeling of failure mechanisms of high power photodetectors. Currently he is working as an Engineer at Microwave Bonding Instruments, Inc. |

| Dr. Nasser. K. Budraa received the Ph.D. in condensed matter physics from the University of California Riverside. Before co-founding MBI, Dr. Budraa was a post- |  |
| --- | --- |
| doctorate fellow at California Institute of Technology and later became an employee of NASA JPL. He performed his research on material bonding initially at JPL. This effort was in concert with his effort on carbon nanotube synthesis and material interaction with microwaves. He is a member of the American Physical Society. |

| Prof. Wen J. Li received the B.S. and M.S. degrees in Aerospace Engineering from USC (in 1987 and 1989, respectively. His industrial experience includes The Aerospace Corporation, Silicon Microstructures Inc., and the NASA/CalTech Jet Propulsion Laboratory. He received the |  |
| --- | --- |
| Aerospace Corporate Fellowship, Silicon Microstructures Inc. Employee Award, and a NASA technical innovation award for his technical contributions to those organizations. He obtained his Ph.D. degree from UCLA in 1997 specializing in MEMS. Prof. Li joined the Department of Automation and Computer-Aided Engineering in 1997. He has since then been active in MEMS and nanotechnology research. In the past six years he has published more than 110 papers in professional journals and conference proceedings on MEMS and nanotechnology related work. Recently, his group's work on nano-sensing and micro-manipulation has received the Best Student Poster Paper Award from the IEEE Nano 2003, and the Best Conference Paper Award from the IEEE ICRA 2003, respectively. Prof. Li is currently the Guest Editor for the Focused Section on Micro and Nano Manipulations of the IEEE/ASME Transactions of Mechatronics, and has also been commissioned to write the chapter on "Nanoscale Robotics and Manipulation" in the Encyclopedia of Nanoscience and Nanotechnology (American Scientific Publishers). Prof. Li is serving as the Director of the Center for Micro and Nano Systems at CUHK, is a member of the Technical Committee on Nanorobotics and Nanomanufacturing of the IEEE Nanotechnology Council, and also a Distinguished Scholar of the Chinese Academy of Sciences. His research interest is to develop micro and nano devices for micro/nano scale sensing and manipulation. |

| Dr. John Mai received a Ph.D. in Aerospace Engineering, with a major field in MEMS, from UCLA (2000). His thesis research involved investigating micro convection cooling. He also received his M.S. (1995) and B.S. (1993) in Aerospace |  |
| --- | --- |
| Engineering from UCLA. He also was a member of the In-situ Exploration Technology Group at the Jet Propulsion Laboratory (1996-2000). He is currently the president of Microwave Bonding Instruments, Inc. |

# Text boxes

(b)

(a)

Hot embossed micro channel

Si substrate with patterned In “grids”

PMMA substrate with patterned Au “rings”

23oC

70oC

(c)

(b)

(a)

(b)

(a)