FABRICATION OF HIGH-ASPECT-RATIO MICRO PIPETTES AND FIBER PROBES

BY SACRIFICIAL BOUNDARY ETCH PROCESS

King W. C. Lai and Wen J. Li*

Centre for Micro and Nano Systems, The Chinese University of Hong Kong,

Shatin, N.T., Hong Kong SAR

ABSTRACT

This paper presents a novel fabrication process to realize high-aspect-ratio micro pipettes and fiber probes which can be used for biological applications. The basic fabrication process employs hydrofluoric acid (HF) to etch the outer layer of the end of capillary tubes and optical fibers as previously reported by other researchers.  However, we invented a “sacrificial boundary etching” technique that can be used to shape micron size tubes and fibers into sharp pipettes or probe tips with controllable tip angle. The tip profile and the length of its taper can be controlled by the initial height of the HF inside a glass tube, which is used as a sacrificial material in shaping the tip profile. Our experimental results showed that capillary tubes and optical fibers can be sharpen into tips with angle as small as 2.1˚ and with tip diameter of ranging from 300 nm to 5 μm (the initial tube and fiber diameter being 125 μm). If the aspect-ratio (AR) of a pipette is defined as the ratio between the length of its taper distance and the length of its base diameter, the AR for our fabricated pipette can be as high as 10.  We also conducted experiments by using the fabricated pipettes to perform microinjection of fluid into cells and fluid ejection to substrates for potential micro-spotting applications.

Keywords: Kwong-Li’s Method, Micro/Nano Pipette, Micro/Nano Injection, Sacrificial Boundary Etching

## INTRODUCTION

The fabrication of micro/nano scale micro pipette and probe has become essential in intracellular surgery. The size of micro probes is a major limitation for micro-cellular operation. For example, to investigate the DNA or small biological tissues in medical sciences, a probe with ultra-small tip diameter is needed. The micropipette has been used in the past but the applications were limited by its size. A summary of micro pipette applications in neural sciences is given in [1]. Currently, the micro pipette is being used in two major ways: 1) it acts as a microelectrode to obtain electrical signal; 2) to perform fluid/substance injection that allows fluid/substance to transfer from one end to the other end which contacts with the cell. Thus, improved technologies for cell sensing, manipulation, or injection could be realized by minimizing the size of these probes and micro pipettes.

On the other hand, Scanning Near-field Optical Microscopy (SNOM) was invented in 1984 to allow potential optical imaging in the nanometer scale. Its spatial resolution can go down to sub-100nm [2], which is far beyond the classical optical microscopy diffraction limit. This promising technique not only has a nanometric resolution, but also retains useful contrast mechanisms in traditional optical microscopy, e.g., polarization and fluorescence [3]. Like all other scanning probe microscopies, probe profile characterizes the resolution of SNOM. In general, the smaller the probe-tip diameter, the better the achievable spatial resolution.  And, the sharper the tip, the smaller the tip angle [4]. Currently SNOM fiber probes are produced by mechanical pulling and chemical etching [3]. Among these, chemically etched probes have a higher optical transmission. Yet, there are limited mechanisms which can easily realize a large range of fabricated probe angles with such high optical transmission.

In this paper, we present a novel probe fabrication process, in which a sacrificial boundary etching technique is combined with a well-known and simple chemical etching process (Turner’s Method [5]). By controlling the initial height of etchant in the sacrificial barrier, final tip profiles were demonstrated to be adjustable. Typical characteristics of probes and micro pipettes etched by this method, such as tip profile, tip diameter and tip angle, are discussed in this paper. Due to the lack of a proper name for this process, we will hence forth call this the KL Method (after its inventors Kwong and Li [6]).

## FABRICATION PRINCIPLE

A simple chemical etching process was introduced by Turner using pure hydrofluoric acid (HF) and organic solvent to fabricate small probe tips from optical fibers [5]. Interfacial meniscus formed between an organic solvent layer and HF which was employed to etch the fibers. We introduced a glass tube as the sacrificial barrier to control the interfacial meniscus precisely as shown in Fig. 1, so that the probe and pipette tip profile can be controlled.

Both the capillary tube and glass tube are held stationary during the fabrication process as shown in Fig. 2a. It is important to align the capillary tube to the center of the glass tube in order to balance the interfacial meniscus surrounding the capillary tube as shown in Fig. 2b. Since HF reacts with the capillary tube and the inner wall of the glass tube continuously, both capillary tube and glass tube would be etched away during the process, so the interfacial meniscus keeps falling. Finally, a micro pipette can be formed with a very long taper and a sharp tip. To control the tip profile, we can simply adjust the initial height of HF in the glass tube at the beginning of the etching process. The final tip profile is also highly depended on the exact etching time.

Fig. 1. Controlling the interfacial meniscus by sacrificial boundary etching. Meniscus geometry changes during the etching process.

Fig. 2. Experimental setup for tip fabrication. a) Capillary tube is dipped perpendicularly to the interfacial meniscus formed by the HF and p-xyene. b) Inset image showing the alignment of the capillary tube.

FABRICATION RESULTS

A set of sacrificial boundary etching experiments was conducted with glass tubes of 21mm inner diameter. Fused silica capillary tubes and optical fibers were the samples used to test the KL Method. Fiber probes were also fabricated by Turner’s Method as reference probes for comparison. In all experiments, single mode fiber was used (F-SA with cladding diameter of 125μm, Newport Corporation) to fabricate fiber probes; flexible fused silica capillary tube was used (TSP002150 with inner diameter of 2 μm and outer diameter of 126 μm, Polymicro Technologies) to fabricate micro pipettes. The difference between the fiber probe and micro pipette is that the micro pipette contains a hollow microchannel which allows fluid to pass through it. The etchant and organic solvent used in the experiments were pure HF (48%) and p-xylene, respectively. These experiments were carried out in 16.5˚C environment, where the typical time for the process was 55 minutes. Our fabricated probe using the above process is compared with a Turner’s probe, an AFM tip and a traditional pulled glass pipette as shown in Fig. 3. Our probes have much smaller tip angle and longer taper than the conventional Turner’s probes used for SNOM. Intuitively, this implies that our fabricated probes can be used to probe or dissect biological cells with much less mechanical resistance on cell membranes. Our micro pipettes would also allow biologists to conduct experiments such as fluid injection with fewer damaging effects to cell membranes.

Fig. 3. SEM pictures of Turner probe, AFM Tip, conventional pipette, and our probes.

MICROPIPETTE TIP PROFILE

The length of taper of the fabricated micro pipette is about 1.5 mm. The tip angle of fabricated micro pipette can be sharpened down to 2.1˚. Examples of various fabricated micro pipette probes are shown in Fig. 4. If the aspect-ratio (AR) of a fabricated micro pipette is defined as the ratio between the length of its tapered distance (L) and the length of its base (W), the AR for a fabricated pipette can be as high as 10. For comparison, Turner’s probes typically have AR ~ 2.

Fig. 4. SEM picture of fabricated micro pipettes with different aspect-ratio.

The cavity at the tip end is also enlarged since HF diffuses into the cavity during the fabrication process as shown in Fig. 5a. However, this diffusion could be prevented by dipping the capillary tube into p-xyene before the process. An improved micro pipette tip is shown in Fig. 5b. For typical fabricated micro pipette as shown in Fig. 6, the inner tip diameter is about 5.5 μm and outer tip diameter is about 6.5 μm. The tip diameter of fabricated micro pipette is limited by the original inner diameter of the capillary tube.

Fig. 5. Microscopic pictures showing the inner microchannel profile of the fabricated micro pipettes: a) HF diffused into the capillary tube; b) without HF diffusion.

Fig. 6. SEM picture of a fabricated micro pipette showing the tip hole. Inset SEM image shows the detailed profile of the tip hole.

The tip angles of fabricated micro pipettes as a function of the initial height of HF is shown in Fig. 7. It implies that increasing the initial height of HF can reduce the tip angle, resulting a sharper pipette tip. The time of the etching experiment will also affect the pipette tip angle as shown in Fig. 7.

Fig. 7. Relationship between tip angles of fabricated micro pipettes and initial height of HF.

## FIBER PROBE TIP PROFILE

Different lengths of the taper of probes were fabricated from etching optical fibers by controlling the initial height of HF. Since the center of optical fibers is a rigid core, tip diameter of fabricated probes can be achieved as small as 300 nm as shown in Fig. 8. It is much smaller than typical tip diameter of Turner’s fiber probes which is about 1μm.

Fig. 8. SEM picture of a fabricated probe tip in nano-scale.

## CELL PROBING EXPERIMENTS

The fabricated nanometric probes and micro pipettes could potentially be used as surgical tools for smaller cells. The comparison between the force of using high aspect-ratio (AR) probes and low (AR) probes when probing cells was performed.

A micromanipulation station with a micro-Newton force sensing system was developed in our prior work [7] to detect force during the micro probing/injection process. The sensing system consists of a PVDF sensor and adapters to a micromanipulator and a probe. We have previously shown that our PVDF sensor could resolve micro-Newton force within a proper frequency range (resonance frequency at ~50Hz and detectable frequency at a few mHz).

In the experiment, we attached the different AR fiber probes to the sensing system to probe and penetrate cells under the control of a 3-axis micromanipulator as shown in Fig. 9.

Fig. 9. Experimental setup for the cell probing experiments.

Fig. 10. High AR probes induced less mechanical force (less voltage sensed) during penetration into a cell.

Unfertilized egg cells of Danio rerio (with diameter ranging from 500μm to 1mm) were employed in our cell probing experiments. The cells were placed on an agarose dish and observed under a microscope. Force signals acquired from penetrating these cells were collected and analyzed. The probing speed of the micromanipulator was set to 1000 μm/s and the travel distance was set to 500 μm. Force sensing signals of low AR probe and high AR probe were obtained and compared as shown in Fig. 10. The founding indicated high AR probe induced less mechanical resistance to the cell, hence, the damage on the cell was minimized. The relationship between the sensor output signal and the probing velocity was discussed in [8]. We also demonstrated the injection of fluids into biological cells using these novel pipettes as shown in Fig. 12.

MICRO-SPOTTING EXPERIMENT

On the other hand, we are also exploring the usage of these pipettes for DNA/protein spotting technology and have shown that solution spot size of 40 μm diameter can be achieved currently as shown in Fig. 11. Since DNA/protein spotting technology requires very fine probe/pipette/ejector to limit the size of DNA solution droplet ejected to the sample substrates, the fabrication process discussed in this paper may be a potential technology to replace existing metal-based probes, which have much larger tip diameters than our probes/pipettes.

Fig. 11. Comparison of droplet size ejected from fabricated pipette and original capillary tube.

## CONCLUSION

A newly invented chemical probe-etching process with high reproducibility was developed which provides a simple, single-step method to fabricate probes with nanometric tips.  With a suitable selection of organic solvent and correct etchant boundary conditions, it is a promising and quick process to fabricate probes for SNOM applications, cell probing and sensing tools, or even cell surgery purposes. In addition, initial experimental analyses were performed on the impact signal between cell membranes and different fabricated probes. The sensed signals clearly indicate that cell membranes will offer finite mechanical resistance even for the nanometric probes during the probing process. Experiments were also conducted for micro-spotting applications and showed that spot size of 40 m is achievable.

## ACKNOWLEDGEMENTS

This project is funded by the Hong Kong Research Grants Council (Grant No. CUHK 4381/02). The authors would like to sincerely thank Ms. Charlotte C. H. Kwong of Mechanical and Aerospace Engineering of UCLA for her contribution to this project.

## REFERENCES

K. T. Brown, D. G. Flaming, “Advanced Micropipette Techniques for Cell Physiology,” IBRO Handbook series: Method in the Neurosciences vol. 9, 1986, pp. 1-6.

B. Hecht, B. Sick, U.P. Wild, V. Deckert, R. Zenobi, O.J.F. Martin and D.W. Pohl, “Scanning Near-field Optical Microscopy with Aperture Probes: Fundamentals and Applications,” Journal of Chemical Physics, 112, 18, 2000, pp. 7761-7774.

P. K. Wong, T.-H. Wang, C.-M. Ho, “Optical Fiber Tip Fabricated by Surface Tension Controlled Etching,” Hilton Head 2002 Solid State Sensor, Actuator and Microsystems Workshop.

A. Klini, T. David, E. Bourillot, S. Emonin, P. Papadopoulos, J.P. Goudonnet, G. Kotrotsios, “Reproducible Optical Fiber Tips for Photon Scanning Tunneling Microsopy with Very Small (<5˚) Cone Angle,” Journal of Lightwave Technology, 16, 7, 1998, pp. 1220-1227.

D. R. Turner, US Patent No. 4,469,554.

C. C. H. Kwong, K. W. C. Lai, and W. J. Li, "Kwong-Li Probes: Novel Nano-Probes for Biological Dissection and Injection," invited paper, IEEE/ASME International Conference on Advanced Intelligent Mechatronics (AIM 2003), Kobe, Japan, July 20-24, 2003, pp. 897 – 901.

C. K. M. Fung, I. Elhajj, W. J. Li, and N. Xi, “A 2-D PVDF Force Sensing System for Micro-manipulation and Micro-assembly,” IEEE ICRA 2002, vol. 2, 2002, pp. 1489-1494.

K. W. C. Lai, C. C. H. Kwong, and W. J. Li, “KL Probes for Robotic-Based Cellular Nano Surgery”, Proc. of IEEE-Nano 2003, Vol. 1, Aug. 12-14, 2003, San Francisco, USA, pp. 152 – 155.

Fig. 12. Inverted microscopic images showing the injection process sequence by using a fabricated micro pipette.

# Footnotes

*Wen J. Li is an associate professor at The Chinese University of Hong Kong and an affiliated professor at the Shenyang Institute of Automation.  This project is funded by The Chinese University of Hong Kong and by the Chinese Academy of Sciences’ Distinguished Overseas Scholar Grant.